## Slide 1
Topological Matter School
August 19th, 2024
Stephen D. Wilson
Professor, Materials Department
University of California, Santa Barbara
Correlations and Topology on Kagome lattices: Lecture 1

## Slide 2: Outline
Introduction to kagome lattice
  Qualitative overview of motivation to study kagome lattice
Kagome lattice Hubbard model
Kagome insulators
  Strong geometric, magnetic frustration
  Quantum spin liquids
Kagome metals
  Strong kinetic, hopping frustration
  Correlated metals

## Slide 3: Introduction to kagome lattice

## Slide 4: Origin of kagome lattice
Bamboo-basket weaving pattern
Kodi Husimi and Itiro Syôzi
Statistical model for spin physics
  Onsager, square lattice
  Temperley, honeycomb lattice
  Wannier, triangular lattice

## Slide 5: Kagome network as 2D tiling motif
11 Archimedean lattices
Tiling of regular polygons with vertices of the same type
Kagome tiling can be thought of as network of corner sharing triangles
Crasto de Lima et al., Phys. Chem. Chem. Phys. (2019)
Smith et al., arXiv:2303.10798 (2023)
*(Not this)

## Slide 6: Kagome lattices in materials
Kagome networks found in many materials
Common example:
  Hexagonal close packed networks
  Make some balls small A2B
  Favored superlattice forms with easy distortion pathways into kagome
Kolii et al., Phys. Rev. Mat. 4, 113604 (2020)
Kolii et al., Acta Materialia 221, 117429 (2021)
Notes: Sqrt3 a x sqrt3 a superlattice favored when big balls and small balls in hcp. This can then distort into kagome

## Slide 7: Kagome lattice Hubbard model

## Slide 8: Kagome band structure
O’Brian et al., Phys. Rev. B 81, 235115 (2010)
Dirac points
flat band
VHS
t
H
K
G
K1
K2
K3
M1
M2
M3
Kagome Brillouin zone

## Slide 9: Two limits: Large and small U
Liu et al., Nature Comm. 11, 4002 (2020)
Imada et al., Reviews of Modern Physics, 70 (1998)

## Slide 10: Kagome insulators

## Slide 11: Magnetic frustration
Real space frustration of AF bonds: J>0
Three sublattice structures
  Triangular lattice + kagome lattice
  Heisenberg triangular lattice orders
  Kagome remains open frontier
  Maximally frustrated lattice in 2D
J
J
J
?
J
J
J
?
?
?
?
?
J
J
J
?
(Extensive degeneracy, unstable to fluctuations)

## Slide 12: Magnetic frustration in two-dimensions
Crasto de Lima et al., Phys. Chem. Chem. Phys. (2019)
Only even sides polygons: unfrustrated
Assuming all equivalent bonds are AF
Lattices with only equivalent bonds versus those with inequivalent
Energy of classical Heisenberg AF and look at energy increase per bond: Triangular and kagome lattice
Richter and Kobe, J. Phys. C (1982) and Quantum Magnetism (Springer)
Strongest quantum fluctuations with largest m and lowest coordination

## Slide 13: Frustrated magnetism in kagome lattices
Gong et al., Physical Review B 91, 075112 (2015)
Rich spectrum of intrinsically quantum disordered and noncoplanar magnetic ground states
Different flavors of spin liquids predicted

## Slide 14: Quantum spin liquid states
Term introduced by Andersen (Mater. Res. Bull. 8 153 (1973))
Highly entangled states of many spins that occur in varying flavors
  Gapless and gapped QSLs
  Gapped QSLs: Topological order and emergent quasiparticles (anyons in 2D)
  Example: Spinon (S=1/2, charge 0 quasiparticle) created in pairs
Savary and Balents, Rep. Prog. Phys. 80 016502 (2017).

## Slide 15: Quantum spin liquid states
Savary and Balents, Rep. Prog. Phys. 80 016502 (2017).

## Slide 16: Unfrustrated magnetism in kagome lattices
Excitations of ordered state can have topogically nontrivial character
Magnons: Bosonic (DS=1) quasiparticles that form a band structure
Etz et al., J. Phys. : Condens. Matter 27, 243202 (2015).

## Slide 17: Unfrustrated magnetism in kagome lattices
Topological magnons in the spectrum of kagome ferromagnets
Three sublattice structure: three magnon bands
Dirac crossing and flat band
Antisymmetric exchange terms (DM interactions) can gap band touching
“Topological magnon insulators”
Chisnell et al., Phys. Rev. Lett. 115, 147201 (2015)

## Slide 18: Materials examples of kagome magnets
Han et al., Nature 492, 406 (2012)
Fractionalized spin excitations
Quantum spin liquid candidate
ZnCu3(OH)6Cl2
Kagome net of Cu2+ (S=1/2) moments
Norman Rev. Mod. Phys. 88, 041002 (2016)

## Slide 19: Materials examples of kagome magnets
Flat magnon band
Gap enhanced
by out-of-plane B-field
Cu(1,3-bdc) (1,3-bdc=1,3-benzenedicarboxylate)
Kagome net of Cu2+ (S=1/2) moments
Nytko et al. Journ. Am. Chem. Soc. 130, 2863 (2008)
Chisnell et al., Phys. Rev. Lett. 115, 147201 (2015)

## Slide 20: Kagome metals

## Slide 21: Different features at different band fillings
Liu et al., Nature Comm. 11, 4002 (2020)
1/3 filling
5/12 filling
3/12 filling
2/3 filling
Dirac point
Two saddle points
Flat band

## Slide 22: One way to visualize kagome band structure
Poincaré-Hopf theorem: Guaranteed 2 saddle points in two dimensional BZ
Bipartite honeycomb lattice

## Slide 23: One way to visualize kagome band structure
Poincaré-Hopf theorem: Guaranteed 2 saddle points in two dimensional BZ
Connect midpoints to form a “line graph”

## Slide 24: One way to visualize kagome band structure
Connection via line graphs: A Mielke J. Phys. A: Math. Gen. 24, ﻿73 (1991).
Populate sites at new vertices
Inherit original bands + flat band

## Slide 25: Kagome lattice near 1/3 filling
Spin-orbit coupling drives Dirac point to gap
Forms strong topological insulator
Quantum spin Hall state
  Bernevig and Zhang , Phys. Rev. Lett. 96, 106802 (2006). Kane and E. J. Mele , Phys. Rev. Lett. 95, 226801 (2005).
Liu et al., Nature Comm. 11, 4002 (2020)
1/3 filling
Guo and Franz, Physical Review B 80, 113102 (2009)
Protected
Edge States

## Slide 26: Kagome lattice near 2/3 filling
2/3 filling
is an eigenstate of the kagome Hamiltonian with
is a compact localized state (akin to a molecular orbital)
Quantum interference
)
Quantum Interference results from kinetic frustration
Localized state results
Graphic courtesy of Riccardo Comin

## Slide 27: Effects at flat band filling
Interactions, in this case, ferromagnetic can generate QAH state
Interactions, in general, are nonpertubative
  Rich spectrum of many-body states

## Slide 28: Flat bands from frustrated hopping
Kagome
Dice
Pyrochlore
+ others…

## Slide 29: Kagome lattice at Van Hove filling
Logarithmic divergent in the local density of states
Léon Van Hove, Phys. Rev. 89, 1189 (1953)
Nesting between VHS can promote electronic instabilities
5/12 filling
3/12 filling
kK
kH
Energy
LDOS

## Slide 30: What can happen when near VH filling?
M2
M3
M1
“Nesting” of electronic states can occur at well-defined wave vector q
Creates peaks in c(q) and c(q) of Lindhard response function
Promotes instabilities, electronic order
Johannes and Mazin, Phys. Rev. B 77, 165135 (2008).
Kabouvand et al, Appl. Phys. Lett. 120, 111901 (2022)

## Slide 31: What can happen when near VH filling?
Mingu Kang et al., Nat. Phys. 18, 301 (2022)
Two flavors of VHS in kagome band structure:
“Pure” VHS with wave functions from a single sublattice
“Mixed” VHS with wave functions from two separate sublattices

## Slide 32: Kagome lattice Hubbard model
Kiesel et al., Phys. Rev. Lett. 110, 126405 (2013).
p-type VHs: U0 diminished/vanishes
“Sublattice interference”
U1 at weak coupling can promote attractive NN site interactions
Unconventional superconductivity predicted to form

## Slide 33: Electronic instabilities at Van Hove filling
Variety of interaction-driven instabilities predicted
  Charge density wave order
  Bond density wave states
  Unconventional superconductivity
Sublattice interference amplifies influence of U1 and extended exchange
Kiesel et al., Phys. Rev. Lett. 110, 126405 (2013).
Wang et al., Phys. Rev. B 87, 115135 (2013).

## Slide 34: Electronic instabilities at Van Hove filling
Chiral flux states
  Orbital antiferromagnets
Primary and secondary orders
  Real and “imaginary” CDW states
Feng et al., Science Bulletin 66, 30 (2021)
Two coupled VHS + NN interactions
Appreciable NNN interaction
Li et al., Phys. Rev. Lett 132, 146501 (2024)
Haldane et al., Phys. Rev. Lett. 61, 2015 (1988)
C M Varma J. Phys.: Condens. Matter 26 505701 (2014)

## Slide 35: How do we find the “right” kagome materials?
Challenge: Dealing with how isolated a kagome net is within a three-dimensional solid
Nearest neighbor distance should be kagome net bonding
Weak bonding in other directions
dK
dNN

## Slide 36: Kagome networks in isolated substructures
Kagome networks not isolated
Kagome networks isolated

## Slide 37: Recent materials survey of kagome compounds
Tolerance factor: t = dk/dNN
dNN
dK
Jovanic and Schoop, J. Am. Chem. Soc. 144, 10978 (2022).

## Slide 38: Also: survey for flat band materials
Regnault et al., Nature 603, 824 (2022).
https://www.topologicalquantumchemistry.com/flatbands/bestflatband.html
https://icsd.fiz-karlsruhe.de/

## Slide 39: Conclusions
Kagome lattices are “target rich” materials platforms for hosting both correlated and topologically nontrivial electronic states
Insulators are near ideal hosts for highly frustrated magnetic order
Metals at various band fillings are predicted to host a variety of unconventional electronic states
Most importantly: Kagome lattices are not uncommon in nature, allows for large range of chemical tunability likely needed to realize/test predicted states