## Slide 1
Topological Matter School
August 19th, 2024
Stephen D. Wilson
Professor, Materials Department
University of California, Santa Barbara
Unconventional Electronic States in Kagome metals, Material Case Studies: Lecture 2

## Slide 2: Outline
Flatband filling materials examples
  Correlation effects, magnetic order
Dirac filling materials examples
  Large AHE, strong Berry curvature
Van Hove Filling materials examples
  Charge density wave order
  Superconductivity
Interfacing kagome nets with other active layers

## Slide 3: Different features at different band fillings
Liu et al., Nature Comm. 11, 4002 (2020)
1/3 filling
5/12 filling
3/12 filling
2/3 filling
Dirac point
Two saddle points
Flat band

## Slide 4: Recent materials survey of kagome compounds
Tolerance factor: t = dk/dNN
dNN
dK
Jovanic and Schoop, J. Am. Chem. Soc. 144, 10978 (2022).
Nearest neighbor distance should be kagome net bonding
Weak bonding in other directions
Chemically two-dimensional a bonus
Be mindful of multiple orbitals, multiple kagome sites

## Slide 5: Kagome metals near flatband fillings

## Slide 6: Kagome lattice near 2/3 filling
2/3 filling
is an eigenstate of the kagome Hamiltonian with
is a compact localized state (akin to a molecular orbital)
Quantum interference
)
Quantum Interference results from kinetic frustration
Localized state results
Graphic courtesy of Riccardo Comin

## Slide 7: Material example 2: FeSn
AF order, unexpected flatband near EF
Do et al., Physical Review B 105, L180403 (2022)
Kang et al., Nature Materials 19 , 163 (2020).

## Slide 8: Material example 1: CoSn
Flat band acquires dispersion near the K point (likely due to NNN hopping)
Flat band at ~ 270 meV binding energy
Kang, Fang, …, JGC, RC, Nature Comm. 11, 4004 (2020)

## Slide 9: Tuning flatband toward EF
Hole-doping sweeps EF through flatband
AF order forms
Sales et al., Chem. Mat. 34, 7069 (2022).

## Slide 10: Material example 3: Ni3In
Flatband crossing EF
Signatures of heavy Fermion behavior/electronic correlations
Ye et al., Nature Physics 20, 610–(2024).

## Slide 11: Kagome metals with gapped Dirac points

## Slide 12: Kagome lattice near 1/3 filling
Spin-orbit coupling drives Dirac point to gap
Forms strong topological insulator
Quantum spin Hall state
  Bernevig and Zhang , Phys. Rev. Lett. 96, 106802 (2006). Kane and E. J. Mele , Phys. Rev. Lett. 95, 226801 (2005).
Liu et al., Nature Comm. 11, 4002 (2020)
1/3 filling
Guo and Franz, Physical Review B 80, 113102 (2009)
Protected
Edge States

## Slide 13: Material example 1: Fe3Sn2 variant
“Bilayer kagome structure”
Some features of kagome band structure preserved
Ferromagnetic order gaps Dirac crossings
Large anomalous Hall effect
Lin et al., Phys. Rev. Lett. 121, 096401 (2018).
Ye et al., Nature 555, 638 (2018).
AHE first noted by:
T Kida et al J. Phys.: Condens. Matter 23, 112205 (2011)

## Slide 14: Material example 2: TbMn6Sn6
Bilayer kagome structure
Interstitial R-site ion forms triangular lattice
Pokharel et al., Phys. Rev. Mat (2023)
Mn
Tb

## Slide 15: Material example 2: TbMn6Sn6
Ferromagnetism, out-of-plane moments
Tb-induced by Mn-moments, strongly uniaxial
Y. X. Yin et al. Nature 583, 533 (2020).

## Slide 16: Kagome metals near VHS

## Slide 17: What can happen when near VH filling?
M2
M3
M1
“Nesting” of electronic states can occur at well-defined wave vector q
Creates peaks in c(q) and c(q) of Lindhard response function
Promotes instabilities, electronic order
Johannes and Mazin, Phys. Rev. B 77, 165135 (2008).
Kabouvand et al, Appl. Phys. Lett. 120, 111901 (2022)

## Slide 18: Material example 1: AV3Sb5 (A=K, Rb, Cs)

## Slide 19: AV3Sb5 (A=K, Rb, Cs) as CDW superconductors
A = Cs, T* = 94 K
A = K, T* = 78 K
A = Rb, T* = 104 K
A = Cs, Tc=2.5 K
A = K, Tc=0.9 K
A = Rb, Tc=0.75 K
Ortiz et al., Phys. Rev. Lett. (2020)
Ortiz et al., Phys. Rev. Mat. (2021)
Yin et al., Chin. Phys. Lett. (2021)

## Slide 20: CDW structure: 2-fold rotational symmetry
Fmmm : 2×2×2 cell
Staggered TrH distortion
Fmmm : 2×2×2 cell
Staggered TrH distortion
Cmmm : 2×2×4 cell
Star of David mixed with tri-hexagonal
CsV3Sb5
RbV3Sb5
KV3Sb5
SoD
TrH
TrH
TrH
SoD
L. Kautzsch et al., Phys. Rev. Mat. (2023)

## Slide 21: Cumulative signs of broken TRS in CDW state
Signatures of broken TRS in a number of probes
  msR, STM, magnetotransport, Kerr, torque, …
Controversies exist in interpretation and reproducibility
Xing et al., Nature (2024).
Piezomagnetic response observed in STM and electron transport: TRS broken but signatures highly impacted by strain
Li et al., Phys. Rev. Lett 132, 146501 (2024)

## Slide 22: Material example 2: RV6Sn6
MgFe6Ge6 structure type
P6/mmm space group
[V3Sn2][RSn1][V3Sn2][Sn3]
  L. Romaka et al. J. All. Comp. (2011)
Ideal V kagome net
Triangular lattice of R-site ions
Affords independent control of R-site magnetism and V-site kagome net
Ganesh Pokharel et al., Phys. Rev. B (2021)

## Slide 23: DFT bandstructure of RV6Sn6
Flat band above ~0.4 above EF
Dirac points at K-point and saddle points at M-point close to EF
Ganesh Pokharel et al., Phys. Rev. B (2021)
YV6Sn6
Multiple magnetic ground states
R=Tb
  Strong uniaxial ferromagnet
  Pokharel et al., PRM (2022)
  E. Rosenberg et al., PRB (2022)
R=Gd
  Incommensurate multi-q order
  Porter et al., PRB (2023)
R=Er, Tm
  Easy-plane AF, no order
  Lee et al., PRM (2022)

## Slide 24: Charge order in ScV6Sn6 (R=Sc)
H. Arachchige et al., Phys. Rev. Lett. (2022)
q=(1/3, 1/3, 1/3)

## Slide 25: Lattice distortion in ScV6Sn6
Tan and Yan, Phys. Rev. Lett. (2023)

## Slide 26: High-temperature charge correlations
type correlations
q=(1/3, 1/3, 1/2)
Pokharel et al., Physical Review Materials, 7, 104201. (2023).
See also: A. Korshunov et al., Nat. Comm. Nature communications 14, 6646. (2023).

## Slide 27: Real space, steric frustration
Primary: Peierls-like distortion of R-Sn-Sn chain
Secondary: Repulsion Sn-Vplane and distortion of kagome net
a
b
a
c
c
a
a
b

## Slide 28: Another example: FeGe
Subires et al., arXiv:2408.04452v1 (2024)
H. Miao et al., Nature Communications 14, 6183 (2023)
Coupled magnetic order and charge order
Chain-like instability between Ge-ions

## Slide 29: Another example: FeGe
Subires et al., arXiv:2408.04452v1 (2024)
High temperature signatures of frustrated dimer formation

## Slide 30: Other examples: Beyond band picture

## Slide 31: Material example 1: (Cs,Rb)Ti3Bi5
D. Verhahn et al., Zeitschrift für Naturforschung B (2022)

## Slide 32: Heavily hole-doped cousin of (Cs,Rb)V3Sb5
D. Verhahn et al., Zeitschrift für Naturforschung B (2022)
No transitions evident down to 80 mK
Useful comparators to (Cs,Rb)V3Sb5
Initially appear to be “boring”, uncorrelated metals

## Slide 33: Hints of hidden symmetry breaking in CsTi3Bi5
Hong Li et al. Nature Physics 19, 1591 (2023),
STM QPI reports 2-fold anisotropy
No rotational symmetry breaking detected in average structure

## Slide 34: Material example 2: Mn3(Sn,Ge) and related
Large room temperature anomalous Hall effect
Associated with real space Berry curvature of noncoplanar magnetic order
Nayak et al., Science advances 2, e1501870 (2016).
Zhang et al., Phys. Rev. B 95, 075128 (2017).
Nakatsuji et al., Nature 527, 212 (2015)

## Slide 35: Large materials space

## Slide 36: Layering Laves into stacked kagome
AB2 into A2B3C
  Split the small spheres into two (B, C)
  Sufficient size difference in B and C orders
  Stacked kagome network results
Relatively unexplored space
  Notable examples in RM3X2
  Ta2V3Si is a recent example (Tc=7.5 K)
Liu et al., Phys. Rev. B 108, 104504 (2023).
MgCu2
Mg2Cu3Si

## Slide 37: Conclusions
Growing number of materials manifestations of some of the key ideas predicted in kagome metals
Materials space is large and, in many cases, highly tunable via chemistry
Future directions in engineering several of these instabilities in the same material platform (e.g. charge order + magnetism or charge order + SC)
Fun chemical ways to trying to create new layered kagome compounds out of three dimensional frameworks